TECHNICAL DATA;  EVERBUILD PINK GRIP SF 


					


DESCRIPTION


PINK GRIP SF  is a direct bond solvent free gap filling adhesive specifically formulated for the professional user.  The product can be used to replace mechanical fixings in a wide variety of building and home improvement applications for bonding wood, brick, plaster, plasterboard, polystyrene, Styrofoam and most plastics, metals and numerous other surfaces. PINK GRIP SF gives the following key benefits.


Enhanced slump resistance for quick and simple direct bonding to most substrates without the use of temporary supports in most applications.


Excellent early and ultimate adhesive strength on porous substrates.


Excellent gap filling properties to accommodate uneven surfaces.


Good “nip off” qualities to prevent messy stringing of the adhesive.


PINK GRIP SF bonds to virtually all common building surfaces to porous substrates and is designed primarily for  internal use.





APPLICATION


The surfaces to be bonded must be clean, dry and totally dust free.  At least one surface must be porous.  Very porous or dusty surfaces should be primed with a PVA sealer and allowed to dry before applying this product. Non porous surfaces must be roughened with sandpaper to improve adhesion.  Cut the tip of the cartridge, pierce the inner membrane and apply using standard sealant gun.





Apply a 6mm diameter bead along the length of the item to be fixed. On large panels, repeat at 600mm centres. Press 


firmly into place and bed down by applying even pressure all over. Very heavy items need to be supported whilst adhesive cures (24-48hrs). When gap filling is necessary, for example battens against an uneven wall, mark the areas where there is a larger gap and apply a thicker bead in these areas.


 Full bond strength is achieved in 24-48 hours.





LIMITATIONS


CAUTION-APPLYING EXTERNALLY.  Do not apply when rain is imminent.  Protect glue line from water contact with impervious paint system or suitable sealant.  In damp or very cold conditions, cure time may be significantly extended.  If in doubt, for external applications, use PINK GRIP.  Do not use where both surfaces are non-porous (e.g. plastic/plastic or metal/metal).  Use a PINK GRIP. Do not use as a mirror adhesive – use MIRROR MATE. It is the user’s responsibility to determine suitability for use.  If in doubt, please contact Technical Services department for advice.





STORAGE


Store in cool, dry conditions between +5 and +25`C. Storage outside these parameters will dramatically reduce shelf life.  Protect from frost.





COVERAGE


Approximately 12 linear meters for a 6mm diameter bead.





SHELF LIFE


Use within 12 months.





HEALTH AND SAFETY





Do not take internally.


Product of low hazardous nature.


Keep out of reach of children.


Dispose of empty packaging correctly.





(EVERBUILD LOGO)


EVERBUILD Building Products Ltd


Site 41, Knowsthorpe Way, Cross Green Industrial Estate, Leeds  LS9 0SW


Tel:	0113 240 3456


Fax:	0113 240 0024						





Rev. 0





Bar Code:	5  029347  60242->


Page � PAGE �1�of � NUMPAGES �1�











