PRODUCT DATA SHEET
 RS500 - ALUMINIUM FOIL TAPE
Description
A 30 micron class ‘o’ aluminium foil Tape with an aggressive solvent acrylic adhesive protected by an easy release liner. It has an excellent peel adhesion as well as being water and fire resistant. Ideal for sealing joints/seams against moisture and vapor. Also suitable for holding, splicing or masking applications requiring protection offered by a foil backing.
Technical Data
Adhesive                                
: Solvent Acrylic
Backing Thickness


: 30 micron
Total Thickness



: 65 micron

Peel Adhesion



: 20 N/25mm

Total Rolling Ball



: 20cm

Tensile Strength



: 37.5 N/25mm

Elongation




: 3.0%

Service Temperature


: -30(C ~ +120(C

Applying Temperature


: +10(C ~ +40(C
The above information is given in good faith and for guidance only. The user shall be responsible for determining that the performance of the product is sufficient for his application. The quoted values are based on averages and should not be taken as maximum or minimum values for specific purposes.
